## Slide 1: Overview of the MIT IHTFP* Loop
*Internally Heated Testloop for PWRs

## Slide 2: Overview of the MIT IHTFP Loop
Circulation Loop
Auxiliary Loop
Controls chemistry
Room temperature, slightly pressurized
Auxiliary Loop
At actual PWR conditions
Where the CRUD actually grows
Circulation Loop

## Slide 3: Main Circulation Loop
Pressure Control
  Increased by pressurizing pump
  Measured by pressure transmitter and gauges
  Set by back-pressure regulator
1
1
2
Temperature Control
  Increased by autoclave heating rod and pre-heater
  Measured by thermocouples in autoclave and on the loop
1
2
2
Flow Control
  Increased by circulation pump
  Measured by differential pressure transmitter
  Moderated by control valve
1
3
3
Fill Terminal
Pressurizing Pump
Pre-heater
Vacuum Terminal
To Vent
Control Valve
Thermocouple
Fill Terminal
To Auxiliary Loop
Autoclave
3
2
    Differential Pressure Sensor
Circulation Pump
Control Valve
Pressure switch
1 Inch tubing
3/4 Inch tubing
1/2 Inch tubing
1/4 Inch tubing
    Pressure Relief Valve
    Pressure Gauge
From Water Tank

## Slide 4: Auxiliary Chemistry Control Loop
Cooler
Drain
Pressurizing pump
pressure
regulator
Small pump
Pressure transmitter
Pressure Gauge
Drain
To Circulation Loop
From Circulation Loop
Ion Exchange Resin Container
Water Tank
Small pump
Temperature Probe
Valve
Flow Sensor
Measurement equipment
pH, Dissolved O2, Conductivity

## Slide 5: Comparison of IHTFP to a PWR
 | PWR | IHTFP
Pressure | 15.5 MPa | 15.5 MPa
Temperature | 287-324°C | 320°C
Reynolds Number | 5 · 105 | 1.62 · 105
Mass flux | 3500 kg/m2s | 1920 kg/m2s
Fe3O4, NiO | 0.01 - 0.1 ppm | 10 - 100 ppm

## Slide 6: Where the Magic Happens: The Autoclave
Sapphire
Windows
Water out
Water in
Actual Autoclave

## Slide 7: First CRUD Growth after One Week
Sample Ring
Flow Ring
    CRUD grown:
      Heater Temperature: 470 Celsius
      Water Temperature: 320 Celsius
      Pressure:155 bars
      7 days
Heater

## Slide 8: CFD Shows Minimal Flow Disturbance
CFD analysis courtesy of Akshay Dave, Victor Petrov, Annalisa Manera of U. Michigan
Flow remains relatively uniform around heating rod

## Slide 9: IHTFP Meshing and Modeling

## Slide 10: IHTFP Simulated Fluid Flow

## Slide 11: IHTFP Simulated Wall Shear Stresses

## Slide 12: CFD-Predicted Quantities

## Slide 13: IHTFP vs. PWR CRUD
Can you tell which is which?

## Slide 14: IHTFP vs. Plant CRUD and Beyond

## Slide 15: Validating MAMBA-BDM Assumptions
Chart: Ln(Box Size)
| 0.69315000000000004 | 1.38629 | 2.07944 | 2.7725900000000001 | 3.4657399999999998 | 4.1588799999999999 | 4.8520300000000001 | 5.5451800000000002 | 6.2383199999999999 | 6.93147
 | 11.5566 | 10.3425 | 9.1813 | 8.0268 | 6.7811 | 5.4116 | 4.0254 | 2.7726 | 1.3863 | 0
 | 20
Fractalline Material Property Models
Wikimedia Commons: “Box Counting Method”

## Slide 16: To Discuss…
What datasets do MAMBA 1D/3D need?
Which conditions predict which phases from thermodynamics? What would you like us to look for?
Can we confirm the CRUD erosion term with coupled MAMBA 3D & CFD?
What else do you want to see?